## Slide 1: CMOS VLSI Design Lecture 18: Variation and Reliability
Notes: Hello and welcome.

## Slide 2: Learning Objectives
At the end of this lecture, you should be able to:
Describe sources and effects of on-chip variation due to process, voltage, temperature and aging.
Outline the major sources of on-chip noise.
Outline the differences between soft and hard errors.

## Slide 3: Variation
Process
  Threshold
  Channel length
  Interconnect dimensions
Environment
  Voltage
  Temperature
Aging/Wearout
Notes: Variation when not taken into consideration during design can cause product delays, respins, yield loss, which may increase the overall cost of production.
Process variation can occur within-die, die-to-die, or wafer-to-wafer. This can cause variance in the performance of circuits due to deviations. The main source of process variations include random dopant fluctuations, line edge roughness, and oxide thickness variation.
Environmental variables include temperature, power supply voltage, which affect the performance of the design during operation, that can be at the user end.

## Slide 4: Process Variation
Threshold Voltage
  Depends on placement of dopants in channel
  Standard deviation inversely proportional to channel area
Channel Length
  Systematic across-chip linewidth variation (ACLV)
  Random line edge roughness (LER)
Interconnect
  Etching variations affect w, s, h
[Bernstein06]
Courtesy Texas Instruments
Notes: Threshold voltage: This source of process variation occurs due to random number of dopant placement in the channel. Increasing the size of the transistor helps in reducing the dopant placement variability.
Channel length: Variation in channel length will reflect on the device output current characteristics and the transistor delay.

## Slide 5: Spatial Distribution
Variations show spatial correlation
  Lot-to-lot (L2L)
  Wafer-to-wafer (W2W)
  Die-to-die (D2D)/inter-die
  Within-die (WID)/intradie
Closer transistors match better
Courtesy M. Pelgrom
Notes: Variation can be die-to-die (D2D), within-die (WID),

## Slide 6: Environmental Variation
Voltage
  VDD is usually designed +/- 10%
  Regulator error
  On-chip droop from
  switching activity
Temperature
  Ambient temperature ranges
  On-die temperature elevated
  by chip power consumption
Courtesy IBM
[Harris01b]
Notes: Environmental variation could be from voltage and temperature.
Unstable voltage supply can lead to undesirable circuit behavior. Source of voltage supply include regulator error, on-chip droop, etc. On-chip droop occurs when gates draw large current from the power supply source during switching.
When circuits operate, the temperature increases due to power consumption. Temperature also has impact on threshold voltage and thermal voltage and resultantly the leakage current.

## Slide 7: Aging
Transistors change over time as they wear out
  Hot carriers
  Negative bias temperature instability
  Time-dependent dielectric breakdown
Causes threshold voltage changes
More on this later…
Notes: Aging occurs over time as transistor wears out due to
hot carriers: Here electron and holes from the channel acquire high kinetic energy, which is enough to inject them in the gate oxide.

## Slide 8: Process Corners
Model extremes of process variations in simulation
Corners
  Typical (T)
  Fast (F)
  Slow (S)
Factors
  nMOS speed
  pMOS speed
  Wire
  Voltage
  Temperature
Notes: Process corners refer to the operating conditions for both nmos and pmos transistors.
In these corners, each transistor could operate in slow, fast, or typical speed.
The factors that affect the operation of a transistor in any of these corners are nMOS speed, pMOS speed, wire, voltage, and temperature.

## Slide 9: Corner Checks
Circuits are simulated in different corners to verify different performance and correctness specifications
Notes: When verifying the performance and correctness of a design, it is usually simulated in different corners.

## Slide 10: Monte Carlo Simulation
As process variation increases, the worst-case corners become too pessimistic for practical design
Monte Carlo: repeated simulations with parameters randomly varied each time
Look at scatter plot of results to predict yield
E.g., impact of Vt variation
  ON-current
  leakage
Notes: In Monte Carlo simulation, a ton of varied random parameters are set as inputs to the design. The computed results enable one to see areas where the design operates nominally.

## Slide 11: Noise
Sources
  Power supply noise/ground bounce
  Capacitive coupling
  Charge sharing
  Leakage
  Noise feedthrough
Consequences
  Increased delay (for noise to settle out)
  Or incorrect computations
Notes: Noise can negatively affect the computation result as well as other factors like increased delay and incorrect computations.

## Slide 12: Reliability
Hard Errors
  Oxide wearout
  Interconnect wearout
  Overvoltage failure
  Latchup
Soft Errors
Characterizing reliability
  Mean time between failures (MTBF)
    # of devices × hours of operation / number of failures
  Failures in time (FIT)
    # of failures / thousand hours / million devices
Notes: Reliability in VLSI depends on a number of factors, which includes hard errors and soft errors.

## Slide 13: Accelerated Lifetime Testing
Expected reliability typically exceeds 10 years
But products come to market in 1-2 years
Accelerated lifetime testing required to predict adequate long-term reliability
[Arnaud08]

## Slide 14: Hot Carriers
Electric fields across channel impart high energies to some carriers
  These “hot” carriers may be blasted into the gate oxide where they become trapped
  Accumulation of charge in oxide causes shift in Vt over time
  Eventually, Vt shifts too far for devices to operate correctly
Choose VDD to achieve reasonable product lifetime
  Worst problems for inverters and NORs with slow input risetime and long propagation delays

## Slide 15: NBTI
Negative bias temperature instability
Electric field applied across oxide forms dangling bonds called traps at Si-SiO2 interface
Accumulation of traps causes Vt shift
Most pronounced for pMOS transistors with strong negative bias (Vg = 0; Vs = VDD) at high temperature

## Slide 16: TDDB
Time-dependent dielectric breakdown
  Gradual increase in gate leakage when an electric field is applied across an oxide
  aka stress-induced leakage current
For 10-year life at 125 C, keep Eox below ~0.7 V/nm

## Slide 17: Electromigration
“Electron wind” causes movement of metal atoms along wires
Excessive electromigration leads to open circuits
Most significant for unidirectional (DC) current
  Depends on current density Jdc (current/area)
  Exponential dependence on temperature
  Black’s Equation:
  Typical limits: Jdc < 1 – 2 mA / μm2
[Christiansen06]

## Slide 18: Electromigration Video

## Slide 19: Electromigration Video 2

## Slide 20: Self-Heating
Current through wire resistance generates heat
  Oxide surrounding wires is a thermal insulator
  Heat tends to build up in wires
  Hotter wires are more resistive, slower
Self-heating limits AC current densities for reliability
  Typical limits: Jrms < 15 mA / μm2
Notes: Current through wires can cause heating. The hotter the wire, the more resistive and slower it gets.

## Slide 21: Overvoltage Failure
High voltages can blow out tiny transistors
Electrostatic discharge (ESD)
  kilovolts from static electricity when the package pins are handled
Oxide breakdown
  In a 65 nm process, Vg ≈ 3 V causes arcing through thin gate oxides
Punchthrough
  High Vds causes depletion region between source and drain to touch, leading to high current flow and destructive overheating
Notes: Electrostatic discharge is the sudden flow of electricity between two electrically charged objects when a conduction path is created. Usually, the direction of current flow is from the object with higher charge to the object with lower charge.
When a strong electric field is applied, this could lead to destruction of an oxide layer. This is known as oxide breakdown.

## Slide 22: Latchup
Latchup: positive feedback leading to VDD – GND short
  Major problem for 1970’s CMOS processes before
  it was well understood
Avoid by minimizing resistance of body to GND/VDD
  Use plenty of substrate and well taps
Notes: Latchup refers to a short circuit formed between power and ground rails.
From the equivalent circuit, when one of the transistors is forward biased, it creates a positive feedback with the other transistor through both bases, and this increases the current flow in the system until the circuit fails.

## Slide 23: Guard Rings
Latchup risk greatest when diffusion-to-substrate diodes could become forward-biased
Surround sensitive region with guard ring to collect injected charge
Notes: Guard rings protect active devices from latchup. For P+ active devices, n+ guard rings are used and vice versa.

## Slide 24: Soft Errors
In 1970’s, DRAMs were observed to randomly flip bits
  Ultimately linked to alpha particles and cosmic ray neutrons
Collisions with atoms create electron-hole pairs in a substrate
  These carriers are collected on p-n junctions, disturbing the voltage
[Baumann05]
Notes: Ionized tracks are formed when high-energy neutrons pass through silicon. These high-energy neutrons may collide with the nuclei of the atoms, which can then drift to form multiple ionized tracks that are diffused in the silicon.
These ionized tracks can create surge in the presence of electric field and change the value stored in the DRAM.

## Slide 25: Radiation Hardening
Radiation hardening reduces soft errors
  Increase node capacitance to minimize impact of collected charge
  Or use redundancy
  E.g., dual-interlocked cell
Error-correcting codes
  Correct for soft errors that do occur
Notes: Electronic components and circuits can be operated in environment with high levels of ionizing radiation. Radiation hardening is making circuits that are resistant to the effects of such hostile environment to prevent damage or malfunction.

## Slide 26: Circuit Pitfalls
Detective puzzle
  Given circuit and symptom, diagnose cause and recommend solution
  All these pitfalls have caused failures in real chips

## Slide 27: Bad Circuit 1
Circuit
  2:1 multiplexer
Symptom
  Mux works when selected D is 0 but not 1.
  Or fails at low VDD.
  Or fails in SFSF corner.
Principle: Threshold drop
  X never rises above VDD-Vt
  Vt is raised by the body effect
  The threshold drop is most serious as Vt becomes a greater fraction of VDD.
Solution: Use transmission gates, not pass transistors

## Slide 28: Bad Circuit 2
Circuit
  Latch
Symptom
  Load a 0 into Q
  Set f = 0
  Eventually, Q spontaneously flips to 1
Principle: Leakage
  X is a dynamic node holding value as charge on the node
  Eventually subthreshold leakage may disturb charge
Solution: Staticize node with feedback
  Or periodically refresh node (requires fast clock,
  not practical processes with big leakage)

## Slide 29: Bad Circuit 3
Circuit
  Domino AND gate
Symptom
  Precharge gate (Y=0)
  Then, evaluate
  Eventually, Y spontaneously flips to 1
Principle: Leakage
  X is a dynamic node holding value as charge on the node
  Eventually subthreshold leakage may disturb charge
Solution: Keeper

## Slide 30: Bad Circuit 4
Circuit
  Pseudo-nMOS OR
Symptom
  When only one input is true, Y = 0.
  Perhaps only happens in SF corner.
Principle: Ratio Failure
  nMOS and pMOS fight each other.
  If the pMOS is too strong, nMOS cannot pull X low enough.
Solution: Check that ratio is satisfied in all corners

## Slide 31: Bad Circuit 5
Circuit
  Latch
Symptom
  Q stuck at 1.
  May only happen for certain latches where input is driven by a small gate located far away.
Principle: Ratio Failure (again)
  Series resistance of D driver, wire
  resistance, and tgate must be much
  less than weak feedback inverter.
Solutions: Check relative strengths
  Avoid unbuffered diffusion inputs where driver is unknown

## Slide 32: Bad Circuit 6
Circuit
  Domino AND gate
Symptom
  Precharge gate while
  A = B = 0; so Z = 0
  Set f = 1
  A rises
  Z is observed to sometimes rise
Principle: Charge Sharing
  If X was low, it shares charge with Y
Solutions: Limit charge sharing
  Safe if CY >> CX
  Or precharge node X too

## Slide 33: Bad Circuit 7
Circuit
  Dynamic gate + latch
Symptom
  Precharge gate while transmission gate latch is opaque
  Evaluate
  When latch becomes transparent, X falls
Principle: Charge Sharing
  If Y was low, it shares charge with X
Solution: Buffer dynamic nodes before
  driving transmission gate

## Slide 34: Bad Circuit 8
Circuit
  Latch
Symptom
  Q changes while latch is opaque
  Especially, if D comes from a faraway driver
Principle: Diffusion Input Noise Sensitivity
  If D < -Vt, transmission gate turns on
  Most likely because of power supply noise or coupling on D
Solution: Buffer D locally

## Slide 35: Summary
Static CMOS gates are very robust
  Will settle to correct value if you wait long enough
Other circuits suffer from a variety of pitfalls
  Tradeoff between performance & robustness
Essential to check circuits for pitfalls
  For large chips, you need an automatic checker.
  Design rules aren’t worth the paper they are printed on unless you back them up with a tool.